**STANSFIELD’S FRAGRANCE OILS LTD**

**Unit 14a**

**Ipark Industrial Estate**

**Innovation Drive**

**Hull**

**HU5 1SG**

**Telephone +44 (0) 1482 447272**

**E-mail info@stansfields.shop**

**CERTIFICATE OF ANALYSIS**

**PRODUCT NAME: LINOSA POLYSORBATE 80**

**BATCH/LOT NUMBER: 356-11**

**Parameters Specifications Results**

Appearance at 25 deg C Clear amber liquid free from foreign matter Conforms

Saponification Value mgKOH/g 45 to 55 51.7

Acid Value mgKOH/g 2 max 0.47

Manufacture Date : 15 January 2020

Retest Date: 15 January 2022

The data listed above constitutes only a technical description of the product. This does not discharge users/consumers from executing a verification of quality and or suitability of the product for the intended use.